## Slide 1
Magnetic Characterization
February 28th 2024
Notes: 1

## Slide 2: Tc
Sample | Tc (K) | ∆Tc (K)
R183-5 | 16.02 | 0.36
R168-5 | 15.83 | 0.3
R173-5 | 15.76 | 0.43
R192-5 | 15.93 | 0.4
R94-4 | 15.23 | 0.3

## Slide 3: Samples with Ta interlayer

## Slide 4: Samples without Ta interlayer

## Slide 5: Upper critical field

## Slide 6: Comparison
No interlayer, of course no Interlayer Annealing, and no Post-Annealing of S.C. Layer
Tc(0) = 16.02 K, μ0HWHH(0) = 16.14 T
R192-5
Interlayer: Ta
Post-Annealing of S.C. Layer
Tc(0) = 15.93 K , μ0HWHH(0) = 15.25 T
S.C. layer thickness = 2.672 μm
S.C. layer thickness = 2.717 μm
Type: Stoichiometric
R183-5
Type: Stoichiometric
R94-4
Interlayer: Ta
Interlayer Annealing
Tc(0) = 15.23 K , μ0HWHH(0) = 21.94 T
S.C. layer thickness = ----
Type: Stoichiometric

## Slide 7: Comparison
No interlayer, of course no Interlayer Annealing, and no Post-Annealing of S.C. Layer
Tc(0) = 16.02 K, μ0HWHH(0) = 16.14 T
R168-5
Interlayer: Ta
No Annealing
Tc(0) = 15.83 K , μ0HWHH(0) = 16.04 T
S.C. layer thickness = 3 μm
S.C. layer thickness = 2.717 μm
Type: Stoichiometric
R183-5
Type: 27%Sn
R173-4
Interlayer: Nb
No Annealing
Tc(0) = 15.76 K , μ0HWHH(0) = 18.84 T
S.C. layer thickness = 2.672 μm
Type: 27%Sn

## Slide 8
Godeke, A. (2006). A review of the properties of Nb3Sn and their variation with A15 composition, morphology and strain state. Superconductor Science and Technology, 19(8), R68.

## Slide 9: Critical current density

## Slide 10: AC measurement

## Slide 11: SHMP

## Slide 12: Measuring Edge